Xiamen JieJing Technology Co.,Ltd. http://www.NaturalHerbalExtracts.com
Room 1201C, Guo Jun Buliding, No.1222, XiaHe Road, Xiamen, China, 361004
Tel : (86)592 8238993  Fax: (86)592 5880308 
Email : Service@NaturalHerbalExtracts.com

# CERTIFICATE OF ANALYSIS

| Product Name | Chitosan | Product Quantity | 1000Kg |  |
| --- | --- | --- | --- | --- |
| Manufacture Date | 2009-03-12 | Batch Code | HL090312F3 |  |
| Specification | Food Grade | Test Date | 2009-03-14 |  |
| Items | Specifications | Results | Results |  |
| Shape＆Properties | white powder solid | white powder solid | Conforms |  |
| Insolubility （%） | ≤1.0 | 0.36 | Conforms |  |
| pH | 7.0-9.0 | 8.7 | Conforms |  |
| Loss on drying（%） | ≤10 | 8.8 | Conforms |  |
| Residue（%） | ≤1.0 | 0.45 | Conforms |  |
| mpa.s Viscosity (1%,20℃) | ≤500 | 40 | Conforms |  |
| D.A.C（%） | ≥90.0 | 95.4 | Conforms |  |
| Mesh size | 80(95%Pass) | Accord | Conforms |  |
| Density，g/ml | ≥0.30 | 0.34 | Conforms |  |
| Conclusion | 该批产品经检验合格 |  |  |  |

Inspector：李平蕊						            Checker：李进国

Date：2009-03-16