Xiamen JieJing Technology Co.,Ltd. http://www.NaturalHerbalExtracts.com
Room 1201C, Guo Jun Buliding, No.1222, XiaHe Road, Xiamen, China, 361004
Tel : (86)592 8238993  Fax: (86)592 5880308 
Email : Service@NaturalHerbalExtracts.com

## CERTIFICATE OF ANALYSIS

| Product Name | Water Soluble Chitosan | Product Quantity | 180Kg |  |
| --- | --- | --- | --- | --- |
| Manufacture Date | 2009.06.22 | Batch Code | 09062201 |  |
| Packing Size | 25kg/纸板桶 | Test Date | 2009.06.29 |  |
| Items | Specifications | Results | Results |  |
| Shape & Properties | white/buff powder | white/buff powder | Conforms |  |
| solubility in water | 在去离子水中溶解 | 符合规定 | Conforms |  |
| Loss on drying（%） | ≤10.0 | 4.2 | Conforms |  |
| Residue（%） | ≤1.0 | 0.1 | Conforms |  |
| pH | 3.0～6.0 | 3.4 | Conforms |  |
| D.A.C（%） | ≥90.0 | 91.5 | Conforms |  |
| Density, g/ml | ≥0.35 | 0.40 | Conforms |  |
| Mesh size | 80(95%Pass) | 符合 | Conforms |  |
| As（mg/kg） | ≤0.5 | 符合规定 | Conforms |  |
| Pb（mg/kg） | ≤1.5 | 符合规定 | Conforms |  |
| Total plate count（cfu/g） | ≤1000 | 已辐照 |  |  |
| Yeast&Mold（cfu/g） | ≤100 | 已辐照 |  |  |
| E.Coli | Negative | 已辐照 |  |  |
| 致病菌 | Negative | 已辐照 |  |  |
| Conclusion | 产品经检验合格，准予出厂。 |  |  |  |

Inspector：李平蕊						            Checker：李进国

Date：06/22/2009